## Slide 1
15 mol% Pu/(U+Pu)
33 mol% Pu/(U+Pu)
Supplementary material: SEM observations of some typical granules constituting the freeze-granulated powders containing 33 and 15 mol% Pu/(U+Pu)

## Slide 2
Supplementary material: Cumulative number frequency of the individual granules constituting the freeze-granulated powders containing 33 and 15 mol% Pu/(U+Pu). The measurements have been done using optical microscopy observations of powder samples positioned on a glass coverslip. Each individual granule projected area is measured and an equivalent two-dimensional disc diameter is calculated (no correction factor). Around 1000 granules are considered for each powder